PRODUCT SPECIFICATION (CSI-FORMAT)

Specifier Note: The specification is in accordance with the Construction Specifications Institute (CSI) format. Please review the specification to meet all specific project requirements and the project evaluation provided by Presto. If an evaluation was not created, please reach out to Bryan Wedin at bryan.wedin@prestogeo.com. Select the appropriate sections shaded in yellow and delete the associated specifier note.

SECTION 31 32 00

SOIL STABILIZATION SYSTEM

PART 1	GENERAL

  - SUMMARY

- Work Included: This section includes providing all material, labor, tools and equipment for installation of geocell system as shown in the Contract Documents and as specified in this section.

- The geocell shall be used for load support application.

  - RELATED SECTIONS AND DIVISIONS

- The applicable provisions of the General Conditions shall govern the work in this Section.

- Section 013300 – Submittal Procedures

- Section 311000 – Site Clearing

- Section 312000 – Earth Moving.

- Section 312500 – Erosion and Sedimentation Control.

- Section 313219 – Geosynthetic Stabilization and Separation Layer.

- Section 323000 - Site Improvements.

- Section 329200 –Turfs and Grasses.

- Section 334600 – Subdrainage.

  - REFERENCES

- American Association of State Highway and Transportation Officials (AASHTO)

- AASHTO M218 – Steel Sheet, Zinc-Coated (Galvanized) for Corrugated Steel Pipe.

- AASHTO M288 – Geotextile Specification for Highway Applications.

- American Society of Testing and Materials (ASTM)

- ASTM D1505 – Density of Plastics by the Density-Gradient Technique.

- ASTM D1603 – Standard Test for Carbon Black in Olefin Plastics.

- ASTM D1693 – Environmental Stress-Cracking of Ethylene Plastics.

- ASTM D5199 – Measuring Nominal Thickness of Geotextiles and Geomembranes.

- ASTM D5394 – Standard Test Method for Environmental Stress-Cracking of Ethylene Plastics.

- ASTM D5596 – Standard Test Method for Microscopic Evaluation of the Dispersion of Carbon Black in Polyoleﬁn Geosynthetics.

- ASTM D 5721 – Standard Practice for Air-Oven Aging of Polyoleﬁn Geomembranes.

- ASTM D 5885 – Standard Test Method for Oxidative Induction Time of Polyoleﬁn Geosynthetics by High-Pressure Differential Scanning Calorimetry.

- ASTM D 6693 (Type IV) – Standard Test Method for Determining Tensile Properties of Nonreinforced Polyethylene and Nonreinforced Flexible Polypropylene Geomembranes.

- ASTM D 7328 – Standard Test Method for Effect of Exposure of Unreinforced Polyoleﬁn Geomembrane Using Fluorescent UV Condensation Apparatus

- ASTM E 41 – Terminology Relating to Conditioning.

- US Army Corps of Engineers (USACE)

  - Technical Report GL-86-19, Appendix A.

- International Organization for Standardization (European Union) (EN-ISO)

  - ISO 6721 – Plastics – Determination of Dynamic Mechanical Properties

  - EN ISO 10319 – Geosynthetics – Wide-Width Tensile Test

  - EN 12224 – Geotextiles and Geotextile-Related Products – Determination of the Resistance to Weathering

  - EN ISO 13426 – Geotextiles and Geotextile-Related Products – Strength of Internal Structural Junctions – Part 1: Geocells

  - EN ISO 13438 – Screening Test Method for Determining the Resistance of Geotextiles and Geotextile-Related Products to Oxidation

  - SUBMITTALS

- Submit manufacturer's shop drawings in accordance with Section 001300, Submittals including Manufacturer’s product data, calculations, drawings and field representative qualifications.

- Manufacturer Calculations. Provide a complete set of project calculations to determine the load support requirements.

- The calculations shall be submitted at the time of bid. The calculation shall be included in an evaluation containing a written summary, plan view, cross section, calculations, stress distribution graph, number of passes graph and research and testing documentation. The evaluation shall be based on site specific project conditions. No standard tables or graphs are acceptable.

- The calculation method shall be based on computer software developed through research and testing at an accredited university or research facility based specifically on the product being submitted.  Provide third party research summary for the calculation method specific to the manufacturer’s material values and panel connectors.

- The load support calculations shall be based on wheel loading, tire pressure, number of passes, bearing capacity coefficient and include the following:

- The minimum allowable stress factor of safety shall be 1.40.

- Provide geocell size and depth.

- Provide hoop stress (psi/kPa) and hoop tension (lb/kg) values.

- Perforated cell wall factor of safety for rupture.

- Internal junction (seams) factor of safety for peel, shear and separation.

- Mechanical junction (panel connection) factor of safety for peel, shear and separation.

- Vertical stress distribution graph showing stress reduction vs. depth below surface.

- Number of passes graph showing cross section requirement vs. number of passes.

- Provide third party testing on panel connection device showing minimum pull through resistance of 275 lbs.

- If required, provide a description of the recommended enhanced woven geotextile separation layer and include in the calculations.

- The stability calculations shall be in Microsoft Excel converted to Adobe PDF format.

- Cross section drawings shall be in AutoCAD converted to Adobe PDF format.

- Manufacturer’s Certificate of Analysis: Manufacturer shall supply certificate of analysis containing the following test results for the geocell material used for project: Base Resin Lot Number(s), Resin Density per ASTM-1505, Production Lot Number(s), Material Thickness, Short Term Seam Peel Strength, and percentage of Carbon Black. Submit qualifications certifying the installer is experienced in the installation of the specified products.

- Submit qualifications of Manufacturer’s field representative certifying the field representative is experienced in the installation of the specified products.

- Submit certificate of compliance that all materials and resins used to produce the specified materials are 100% made by plants located in the United States per public law Build America, Buy America (BABA) included in the Infrastructure Investment and Jobs Act under Title IX, Subtitle A, Part 1.

- No material will be considered as an equivalent to the geocell material specified herein unless it meets all requirements of this specification, without exception. Manufacturers seeking to supply what they represent as equivalent material must submit records, data, independent test results, samples, certifications, and documentation deemed necessary by the Engineer to prove equivalency. The Engineer shall approve or disapprove other Manufacturers’ materials in accordance with the General Conditions after all information is submitted and reviewed. Any substitute materials submitted shall be subject to independent lab testing at the contractor’s expense.

  - QUALITY ASSURANCE AND CONTROL

- The geocell material shall be provided from a single Manufacturer for the entire project.

- The Manufacturer’s Quality Management System shall be certified and in accordance with ISO 9001:2015 and CE certification. Any substitute materials submitted shall provide a certification that their geocell manufacturing process is part of an ISO program and a certification will be required specifically stating that their testing facility is certified and in accordance with ISO. An ISO certification for the substitute material will not be acceptable unless it is proven it pertains specifically to the geocell manufacturing operations.

- The Manufacturer shall provide certification of compliance to all applicable testing procedures and related specifications upon the customer’s written request. Request for certification shall be submitted no later than the date of order placement. The Manufacturer shall have a minimum of 20 years’ experience producing geocells and accessories.

- Pre-Installation Meeting: Prior to installation of any materials, conduct a pre-installation meeting to discuss the scope of work and review installation requirements. The pre-installation meeting shall be attended by all parties involved in the installation of the geocell.

- Manufacturer’s Field Representative Qualifications:

- Manufacturer shall provide a qualified field representative on site at the start of construction to ensure the system is installed in accordance with the Contract Documents.

- Manufacturer’s field representative shall have a minimum 5 years’ installation experience with the specified products in the specified application.

- Manufacturer of any substitute materials to be used shall certify that a representative can meet the above criteria and will be on site for initial construction start up. Manufacturers other than Presto will be required to provide proof the representative meets these qualifications.

  - DELIVERY, STORAGE, AND HANDLING

- Deliver materials to site in Manufacturer’s original, unopened containers and packaging, with labels clearly identifying product name and Manufacturer.

- The materials shall be stored in accordance with Manufacturer’s instructions. The materials shall be protected from damage and away from direct sunlight.

- The materials shall be delivered, unloaded and installed in a manner to prevent and minimize damage.

  - WARRANTY

- The Manufacturer shall warrant each section that it ships to be free from defects in materials and workmanship at the time of manufacture. The Manufacturer’s exclusive liability under this warranty or otherwise will be to furnish without charge to the original f.o.b. point a replacement for any section which proves to be defective under normal use and service during the 10-year period which begins on the date of shipment. The Manufacturer reserves the right to inspect any allegedly defective section in order to verify the defect and ascertain its cause.

- This warranty shall not cover defects attributable to causes or occurrences beyond the Manufacturer’s control and unrelated to the manufacturing process, including, but not limited to, abuse, misuse, mishandling, neglect, improper storage, improper installation, improper alteration or improper application.

- In no event shall the Manufacturer be liable for any special, indirect, incidental or consequential damages for the breach of any express or implied warranty or for any other reason, including negligence, in connection with the geocell.

PART 2	PRODUCTS

2.1	ACCEPTABLE MANUFACTURER

A.	Presto Geosystems, PO Box 2399, Appleton, Wisconsin 54912-2399.

Phone: (920) 738-1328. Email: info@prestogeo.com. Website: www.prestogeo.com.

2.2	GEOWEB® GEOCELL

- Manufacturing Certification

- The Manufacturer shall have earned a certificate of registration, which demonstrates that its quality-management system for its geocell is currently registered to the ISO 9001:2015 and CE quality standards.

- Base Materials

- Polyethylene Stabilized with Carbon Black

- Density shall be 58.4 to 60.2 pound/ft3 (0.935 to 0.965 g/cm3) in accordance with ASTM D1505.

- Environmental Stress Crack Resistance (ESCR) shall be 5000 hours in accordance with ASTM D1693.

- Resistance to Oxidation shall be minimum of 100 years in accordance with EN ISO 13438.

- 100% of original strip tensile strength shall be retained following exposure to accelerated weathering in in accordance with EN 12224.

- The Flexural Storage Modulus shall be a minimum of 800 MPa in accordance with ISO 6721.

- Ultra-Violet light stabilization with carbon black.

- Carbon Black content shall be 1.5 to 2 percent by weight, through addition of a carrier with certified carbon black content.

- Carbon black shall be homogeneously distributed throughout material.

- The manufacturer must have an in-place quality control to prevent irregularities in strip material.

- Cell Properties

    - Individual cells shall be uniform in shape and size when expanded.

    - Individual cell dimensions (nominal) shall be dimensions  10%.

Specifier Note: Select the appropriate cell size and depth recommended in the project evaluation and delete the others.

    - GW20V Cell

      - Length shall be 8.8 inches (224 mm).

      - Width shall be 10.2 inches (259 mm).

      - Nominal area shall be 44.8 in2 (289 cm2) plus or minus 1%.

      - Nominal depth shall be [8 inches (200 mm)] [6 inches (150 mm)] [4 inches (100 mm)] [3 inches (75 mm)].

    - GW30V Cell

      - Length shall be 11.3 inches (287 mm).

      - Width shall be 12.6 inches (320 mm).

      - Nominal area shall be 71.3 in2 (460 cm2) plus or minus 1%.

      - Nominal depth shall be [8 inches (200 mm)] [6 inches (150 mm)] [4 inches (100 mm)] [3 inches (75 mm)].

- Strip Properties and Assembly

- Perforated Textured Strip/Cell

- Strip sheet thickness shall be 50 mil (1.27 mm), minus 5 percent, plus 10 percent in accordance with ASTM D5199. Determine thickness flat, before surface disruption.

- Polyethylene strips shall be textured surface with a multitude of rhomboidal (diamond shape) indentations.

- Textured sheet thickness shall be 60 mil plus or minus 6 mil (1.52 mm plus or minus 0.15 mm).

- Indentation surface density shall be 140 to 200 per in2 (22 to 31 per cm2).

- Perforated with horizontal rows of 0.4-inch (10 mm) diameter holes.

- Perforations within each row shall be 0.75 inches (19 mm) on-center.

- Horizontal rows shall be staggered and separated 0.50 inches (12 mm) relative to hole centers.

- Edge of strip to nearest edge of perforation shall be a minimum of 0.3 inches (8 mm).

- Centerline of spot weld to nearest edge of perforation shall be a minimum of 0.7 inches (18 mm).

- A slot with a dimension of 3/8 inch x 1-3/8 inch (10 mm x 35 mm) is standard in the center of the non-perforated areas and at the center of each weld.

- Assembly of Cell Sections

  - Fabricate using strips of sheet polyethylene each with a length of 142 inches (3.61 m) and a width equal to cell depth.

  - Connect strips using full depth ultrasonic spot-welds aligned perpendicular to the longitudinal axis of strip.

  - Ultrasonic weld melt-pool width shall be 1.0-inch (25 mm) maximum.

Specifier Note: Select the appropriate cell size recommended in the project evaluation and delete the others.

  - Weld spacing for GW20V cell sections shall be 14.0 inches plus or minus 0.10 inch (356 mm plus or minus 2.5 mm).

  - Weld spacing for GW30V cell sections shall be 17.5 inches plus or minus 0.10 inch (445 mm plus or minus 2.5 mm).

- Cell Seam Strength Tests

1.	Minimum seam strengths are required by design and shall be reported in test results. Materials submitted with average or typical values will not be accepted. Written certification of minimum strengths must be supplied to the engineer at the time of submittals.

2.	Short-Term Seam Peel-Strength Test

- Cell seam strength shall be uniform over full depth of cell.

Specifier Note: Select the appropriate cell depth recommended in the project evaluation and delete the others.

- Minimum seam peel strength shall be [640 lbf (2,840 N) for 8-inch (200 mm) deep panels] [480 lbf (2,130 N) for 6-inch (150 mm) deep panels] [320 lbf (1,420 N) for 4-inch (100 mm) deep panels] [240 lbf (1060 N) for 3-inch (75 mm) deep panels].

- Long-Term Seam Peel-Strength Test

- Conditions:  Minimum of 7 days in a temperature-controlled environment that undergoes change on a 1-hour cycle from room temperature to 130 °F (54 °C).

- Room temperature shall be in accordance with ASTM E41.

- Test samples shall consist of two, four-inch (100 mm) wide strips welded together.

- Test sample consisting of two carbon black stabilized strips shall support a 160-pound (72.5 kg) load for test period.

- Internal Junction Efficiency

  - Internal junction efficiency (seams) shall be determined as a ratio of junction performance to perforated strip performance, as determined by EN ISO 10319 and EN ISO 13426.

  - Internal junction efficiency (factor of safety) shall be calculated for peel, shear and separation.

  - Minimum internal junction efficiency shall be ≥ 100 percent.

- Mechanical Junction Efficiency

  - Mechanical junction efficiency (panel to panel connection) shall be determined as a ratio of junction performance to perforated strip performance, as determined by EN ISO 10319 and EN ISO 13426.

  - Mechanical junction efficiency (factor of safety) shall be calculated for peel, shear and separation.

  - Minimum mechanical junction efficiency shall be ≥ 100 percent.

  - Panel connection device shall be with integral components as designed by the Manufacturer.

- 10,000-hour Seam Peel Strength Certification

  - Provide data showing that the high-density polyethylene resin used to produce the geocell sections has been tested using an appropriate number of seam samples and varying loads to generate data indicating that the seam peel strength shall survive a loading of at least 209 lbf (95 kg) for a minimum of 10,000 hours.

  - INTEGRAL COMPONENTS

- ATRA® Stake Clip

- The stake clip is a molded, high-strength polyethylene device available in standard (0.5 inch) and metric (10–12 mm) versions.

- Stake clips shall be installed as an end cap on No. 4 (0.5 inch) and metric (10–12 mm) steel rebar to form ATRA® Anchors.

- ATRA® Key

- The keys shall be constructed of polyethylene and provide a high strength connection with minimum pull-through resistance of 275 lbs (125 kg).

- Keys shall be used to connect sections together at each interleaf and end-to-end connection.

- The keys include a structurally reinforced handle and frictional barbs to enhance interlock with the textured wall surface to prevent mechanical joint failure including peel, shear and separation.

- Metal staples, zip ties, and two-piece connectors are not an acceptable panel connection method.

  - STAKE ANCHORAGE

Specifier Note: If applicable, select the appropriate stake anchorage recommended in the project evaluation and delete the others. If stake anchorage is not recommended, delete entire section.

- ATRA® Anchors

- Anchors shall consist of No. 4 (0.5 inch) or metric (10–12 mm) steel reinforcing rod with a stake clip attached as an end cap.

- Anchors shall be assembled by inserting the stake clip onto the rebar so that the end is flush with the top of the stake clip. Prior to attaching the stake clip, the rebar shall be beveled and free from all burrs.

- The anchor length and placement shall be as shown in the Contract Documents.

- ATRA® Speed Stake

- Speed stake shall be one piece injected molded design with integral flanged arms and barbs.

- The stake shall be constructed of a specialty-based HDPE polymer alloy.

- The minimum tensile strength shall be 14.5 kips (100 mPa).

- The minimum bending strength shall be 575 lbs (2.55 kN).

- The stake shall be non-magnetic, non-conducting and corrosion resistant.

- The stake length and placement shall be as shown in the Contract Documents.

  - INFILL MATERIALS

Specifier Note: Select the appropriate infill material recommended in the project evaluation and delete the others. Add the appropriate infill material if not included below.

- Infill material shall be coarse sand with maximum fines content of 15%.

- Infill material shall be crushed aggregate with a maximum particle size of one-third cell depth.

- Infill material shall be recycled materials with a maximum fines content of 15% and particle size of one-third the cell depth.

- Infill material shall be concrete with a minimum strength of 3000 psi and air content of 2 to 4% in accordance with ACI and ASTM standards. The slump should be adjusted in the field to allow installation.

- Infill material shall be an engineered fill consisting of topsoil and aggregate mixture for vegetated surfaces.

- Engineered infill shall consist of 1/3 pulverized topsoil and 2/3 aggregate mixture. The mixture shall promote vegetation growth and provide structural support.

- The aggregate portion shall have a particle range from 0.375 to 1.0 inches (9.5 to 25 mm) with a D50 of 0.5 inches (13 mm).

- Blend the topsoil and aggregate to produce a homogenous mixture.

- The percentage void space of the aggregate portion when compacted shall be at least 30%.

- Once placed, the mixture shall be compacted in accordance with Contract Documents.

- Infill material shall be free of any foreign material.

- Clays and silts are not acceptable infill material.

- Infill material shall be free-flowing and not frozen when placed in the sections.

  - ADDITIONAL COMPONENTS

Specifier Note: If applicable, select the appropriate additional components recommended in the project evaluation and delete the others.

- Surface Protection

- Surface protection shall consist of [hydroseed] [erosion control blanket] [turf reinforcement mat] as specified in the Contract Documents.

- Geotextile

- The non-woven OR enhanced woven geotextile separation layer shall be as specified in the Contract Documents.

PART 3	EXECUTION

  - EXAMINATION

- Verify site conditions are as indicated on the drawings. Notify the Engineer if site conditions are not acceptable. Do not begin preparation or installation until unacceptable conditions have been corrected.

- Verify layout of structure is as indicated on the drawings. Notify the Engineer if layout of structure is not acceptable. Do not begin preparation or installation until unacceptable conditions have been corrected.

  - INSTALLATION

- Prepare subgrade and install load support system in accordance with Contract Documents and manufacturer's installation guidelines.

Specifier Note: Revise the installation assistance as required including days on site and number of trips.

- On-site time for installation assistance by the Manufacturer’s field representative shall be a minimum of a 1 day with one trip. All travel and expense costs for field representative installation observation shall be included in the base bid price.

- Subgrade Preparation

- Excavate and shape sub grade in accordance with the Contract Documents.

- Ensure foundation soil meets minimum strength requirements through proof rolling or other conventional method and is approved by the Engineer. If unacceptable foundation soils are encountered, excavate and replace with suitable quality material as directed by the Engineer.

- Install geotextile separation layer in accordance with the Contract Documents and manufacturer’s recommendations including overlaps based on sub grade CBR.

- Subbase Preparation and Installation

- Ensure that the subgrade soil meets the minimum strength requirements for installation of the subbase.

- Place additional subbase materials to the required depth as specified in the Contract Documents.

- Compact to a minimum 95 percent Standard Proctor.

- Install geotextile separation layer on top of subbase ensuring required overlaps are maintained and outer edges of the geotextile are buried in accordance with the Manufacturer’s recommendations.

- Section Anchorage and Connection

- Anchorage requirements shall be as shown on the Contract Documents.

Specifier Note: Select the appropriate section anchorage recommended in the project evaluation and delete the others. Revise wear surface if different than 2 inches.

- Anchorage shall be provided by ATRA anchors or ATRA speed stakes.

- After the sections are expanded, drive anchors or speed stakes so the arm of the stake clip engages with the top of the cell wall.

- Connect the sections with keys at each interleaf and end-to-end connection. Insert the key through the cell wall I-slot before inserting through the adjacent cell. Turn the key 90 degrees to lock the sections together.

- Anchorage pattern and stake length shall be as specified in the Contract Documents.

- Coarse Sand Infill Placement

- Place infill with suitable material handling equipment.

- Infill material shall be free-flowing and not frozen when placed in the sections.

- Overfill cells and compact to provide a minimum 2-inch wear surface. Maintain the wear surface over the sections to prevent damage to the cell walls.

- Limit the drop height to prevent panel distortion.

- Compact as specified in the Contract Documents.

- Aggregate Infill Placement

- Place infill in expanded cells with suitable material handling equipment.

- Infill material shall be free-flowing and not frozen when placed into the sections.

- Overfill cells and compact to provide a minimum 2-inch wear surface. Maintain the wear surface over the sections to prevent damage to the cell walls.

- Limit the drop height to prevent panel distortion.

- Compact as specified in the Contract Documents.

- Recycled Material Infill Placement

1.	Place infill in expanded cells with suitable material handling equipment.

2.	Infill material shall be free-flowing and not frozen when placed into the sections.

3.	Overfill cells and compact to provide a minimum 2-inch wear surface. Maintain the wear surface over the sections to prevent damage to the cell walls.

4.	Limit the drop height to prevent panel distortion.

5.	Compact as specified in the Contract Documents.

- Concrete Infill Placement

- Place infill with suitable material handling equipment. Concrete shall be placed, finished and cured in accordance with the Contract Documents.

- Once infill begins, infilling shall be continuous until a designated section is completed or as approved by the Engineer.

- Limit the drop height to prevent panel distortion.

- The concrete shall be vibratory compacted in accordance with the Contract Documents.

- Concrete shall be screeded flush with the top of the walls. Apply specified finish.

- Engineered Infill Placement

- Place infill with suitable material handling equipment.

- Infill shall be free-flowing and not frozen when placed in the sections.

- Overfill cells and compact to provide a minimum 2-inch wear surface. Maintain the wear surface over the sections to prevent damage to the cell walls.

- Limit the drop height to prevent panel distortion.

- Compact as specified in the Contract Documents.

- Surface protection shall be provided and installed in accordance with the Contract Documents.

# Appendix A

## Short-Term Seam Strength Test Procedure

### Frequency of Test

Figure A1

The short-term seam peel strength test (referred to as the ‘test’ in this section) shall be performed on a geocell section randomly taken directly from the production line each two hours.

### Test Sample Preparation

Randomly choose 10 welds within the selected section and cut those welds from the section such that 10 cm (4 in) of material exist on each side of the weld. The test sample shall have a general appearance as illustrated in Figure A1. Prior to testing, the test samples shall have air cool for a minimum of 30 minutes from the time the selected geocell section was manufactured.

### Short-term Seam Peel Strength Test

The apparatus used for testing the short-term seam peel strength shall be of such configuration that the jaws of the clamp shall not over stress the sample during the test period. Load shall be applied at a rate of 12 in (300 mm) per minute and be applied for adequate time to determine the maximum load. The date, time and load shall be recorded.

Short-term seam peel strength shall be defined as the maximum load applied to the test sample. Minimum required short-term seam peel strength shall be:

640 lbf (2840 N) for the 8 in (200 mm) depth cell

480 lbf (2130 N) for the 6 in (150 mm) depth cell

320 lbf (1420 N) for the 4 in (100 mm) depth cell

240 lbf (1060 N) for the 3 in (75 mm) depth cell.

### Definition of Pass / Failure

Two methods shall be used to determine acceptability of the manufactured geocell sections. The successful passing of the short-term seam peel test shall not be used to determine acceptable of the polyethylene for use in manufacturing of the geocell sections. Acceptability of the polyethylene shall be determined through tests conducted in Appendix B.

### The Tested Value

If more than one of the tested seam samples fails to meet the minimum peel strength, all sections manufactured after the previously successful test shall be rejected.

If all tested seam samples meet the minimum peel strength, all geocell sections manufactured since the last successful test shall be considered to have passed the test.

When one of the tested seam samples fails to meet the minimum peel strength, another 10 samples shall be randomly selected and cut from the previously selected section. If more than one of these samples fails, all sections manufactured after the previously successful test shall be rejected. Otherwise, all geocell sections manufactured since the last successful test shall be considered to have passed the test.

### Visual Failure Mode

After each sample is tested, the seam shall be examined to determine the failure mode. Two failure modes are possible.

Material failure within and adjacent to the weld indicated by material strain and

Weld failure resulting in complete separation of the seam and shows little or no material strain.

Upon examination, when the failure mode results in complete separation of the seam and indicates little or no material strain, product manufactured shall be rejected.

# Appendix B

## Long-Term Seam-Strength Test Procedure

### Frequency of Test

Figure B1

The long-term seam peel strength test (referred to as the ‘test’ in this section) shall be performed:

- On each new resin lot number if the geocell manufacturer extrudes the sheet or strip used to produce the geocell material.

- On each new order of sheet and/or strip if the geocell manufacturer does not extrude the sheet and/or strip used to produce the geocell material.

### Test Sample Preparation

A test sample shall be made using two sets of two strips meeting all aspects of the material portion of this specification. Testing shall be done on non-perforated samples to obtain the true seam strength of the bond. One set of two strips are to be welded in welder position “A” and the other set of two strips are to be welded in welder position “B” producing two 1-cell long sections of geocell product. Welding should be done using a warm welder. The welded samples shall be labeled “A” and “B” and the weld seams of each sample shall be numbered consecutively from left to right starting with the number 1 (one) and corresponding to the welding head number.

The samples shall air cool for a minimum of 30 minutes. Randomly choose 10 welds from samples “A” and “B” and cut those welds from the geocell samples such that 4 in (10 cm) of material exist on each side of the weld. These samples shall be cut to a width of 4 in (10 cm). Properly identify each weld using the sample letter and weld seam number.

These samples are now ready to be tested.

### Long-term Seam Peel Strength Test

The long-term seam peel strength test shall take place within an environmentally controlled chamber that undergoes temperature change on a 1-hour cycle from room temperature to 130°F (54°C). Room temperature shall be defined per ASTM E41.

Within the environmentally controlled chamber, one of the ends of the samples (10 samples in total) shall be secured to a stationary upper clamp. The jaws of the clamp shall be of such configuration that the grip does not over stress the sample during the test period. The sample shall be secured so that its axis is vertical and the welds being tested are horizontal as the sample hangs within the environmentally controlled chamber.

A weight of 160 lb (72.5 kg) shall be lifted via a hoist or lift platform and attached to the free lower end, of the sample. The weight shall be lowered in a way so that no impact load occurs on the sample being tested. The weight shall be sufficient distance from the floor of the chamber so that the weight will not touch the floor of the chamber as the sample undergoes creep during the test period. The date and hour the weight is applied shall be recorded.

The temperature cycle shall commence immediately within the environmentally controlled chamber. The test period for the applied load shall be 168 hours.

### Definition of Pass / Failure

If any of the 10 seams fail prior to the end of the 168-hour (7-day) period, the date and hour of the failure shall be recorded and the polyethylene resin and strip material shall be considered unsuitable for geocell manufacturing.

END OF SECTION